Mipolam Elegance EL5

MIPOLAM ELEGANCE EL5 is a conductive flexible homogeneous vinyl floorcovering available in sheet form.

The 2 mm homogeneous material incorporates carbon encapsulated granules throughout its full thickness and has a conductive backing to ensure optimal and consistent conductive properties throughout its full life expectancy.

It has permanent antistatic properties (< 20 V).

This floorcovering is treated with Evercare™ or the latest improvements in polyurethane surface treatment obtained by UV laser cross-linking. Evercare™ avoids staining of chemical products used in healthcare like betadine, eosin or anti-bacterial hand gel and increases the durability of the flooring.

This treatment has excellent maintenance characteristics; it requires no wax for life!

MIPOLAM ELEGANCE EL5 acts as a continuous conductive 5.104 ≤ Rt ≤ 106 (EN 1081) and complies with EN 649.

The product is non-reactive to residual indentation with a value ≤ 0,02 mm (EN 433)

The flooring complies with the EN 649 (34-43) offering a group P wear rating suitable for heavy duty traffic areas and Bfl-s1 fire resistance.

The product is non-emissive of volatile organic compounds with <10 µg/m3 (TVOC after 28 days ISO 16000-6).