# 

**TARALAY IMPRESSION ACOUSTIC**

TARALAY IMPRESSION ACOUSTIC 0,65 is a multi-layered vinyl floorcovering, integrating a **Very High Density foam backing**, reinforced with a fiber glass and a printed design. It’s available in 2 m wide sheet, with a group T wear rating.

Total width of the product is  **3,35 mm,** including a transparent wear layer of 0.65 mm thick. It offers **19 dB sound insulation** and an **indentation resistance of ca. 0.08 mm.** Its **dimensional stability** performs down to **0,08%** (average measure).

TARALAY IMPRESSION ACOUSTIC is made in France, with green electricity. It’s **100% recyclable**, and the floorcovering will have its individual EPD sheet.

The flooring is equipped with **Protecsol® 2**, patented surface treatment obtained by UV laser cross-linking offering the best chemical resistance to the main products used in healthcare environment as betadine, eosin, hydro alcoholic solutions, making the maintenance easy and the floor long lasting. This treatment avoids applying any acrylic emulsion throughout the lifetime of the product.

It is **free of formaldehyde**, **heavy metals** and **CMR 1 & 2 or vPvB** (very persistent and very bio accumulative) or PBT (persistent, bio-accumulative and toxic) and is 100% REACH compliant. Its VOC emissions after 28 days (ISO 16000-6) are below detection levels (<10 μg / m3) and this product is classified A + (the best class) and Floorscore® & M1 certified for indoor air quality. Taralay Impression Compact has antibacterial efficacy (E.coli / S.aureus / MRSA) : >99% after 24 hours according to ISO22196.