**CREATION 40 TREND** is a synthetic, decorative, flexible, antistatic abrasion group T floorcoverings available in tile or plank, with bevelled edges. It consists in a 0,4 mm thick transparent wear layer, a design film and a Resilient Comfort Core to provide softness and comfort surface. The overall thickness is 2 mm.

They benefit from a cross-linked polyurethane surface treatment (ProtecshieldTM), making maintenance easier and prevent from micro scratches.

**CREATION 40 TREND** is a glued floorcovering, resistant to use (residential / commercial use) of 23 / 32 according to EN-ISO 10874 and has Bfl -s1 class for smoke emission according to EN 13501-1.

**CREATION 40 TREND** is made with phthalate free plasticizers, except recycled content. It is 100% recyclable and made with 35% of recycled content. It is 100% compliant with REACH. The product emission rate of organic compounds is < 10 micrograms/m3 (TVOC <28 days – ISO 16000-6).